Table S1: Study Characteristics

| Abbreviation | Full name |
| --- | --- |
| LAK | Lake |

| Reference | Country | Source | Treatment | Sampling Date | Size, shape | Polymers, chemicals | Value | Detection limit, negative and positive controls and blanks. | Sampling method | Analysis method | Comments |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Anderson et al. 2017 | Lake Winnipeg, Canada | LAK | n.a. | Jul 2014 - Jun 2016 | Fibres, fragments, film and foam (pellets not found). | n.i. | Mean: 193 420 (±115 567 SD) #/km2 Range: 52 508 – 748 027 #/km2 | DI water blanks (quadruplicates, 480L). Air blanks for 24h. Corrected for both blanks. | Manta trawl; 333 m mesh. Preserved in 70% ethanol. | Samples rinsed and large objects removed; WPO treatment with Fe(II), heated to 75 °C; visual inspection of subsamples for plastics; subset of particles identified with SEM-EDS. |  |
| Baldwin et al., 2016 | Great Lake tributaries, US | RIV | n.a. | Apr 2014 - Apr 2015 | Size: 0.355-0.999, 1.00-4.759, ≥4.75 mm; Shape: Fragments, pellets/beads, lines/fibers, films and foam. | n.i. | Mean: 4.2 x 10-3 #/L; Median: 1.9 x 10-3 #/”L; Range: 0.05 - 32 (x10-3) #/L | Five negative controls in the field and 11 in the lab were included. | Neuston net (333 µm). Sample volume measured. . Net rinsed with tap water or filtered (333 µm) stream water. Preserved in isopropyl alcohol. | Sieving through 4.75, 1.00 and 0.355 mm mesh. WPO with Fe(II) catalyst at 75°C). WPO solution sieved through 125 µm and MP visually identified under dissection microscope (40x). |  |
| Mason et al. 2018 | US and others | BOT | n.a. | 2017 | Size: 6.5-100, >100 µm; Shape: Fragment, film, fibre, foam, pellet | PP, nylon, PS, PE, PEST | Mean: 325 #/L (> 100 m - 10.4 #/L, < 100m - 315 #/L); Range: 0-10390 #/L | Lab blanks included. | Bottles opened in laminar flow hood and Nile Red dye added. | Filtered on glass fibre filter; fluorescence microscopy; FTIR on a subset. |  |
| Faure et al. 2015 | Lake Geneva and rivers, CH | LAK, RIV | n.a. | 2013 | Size: 300 – 5000 µm. Shape:Fragments, pellets, beads, lines, fibres, films, foams. | PE, PP, PS | Lakes: Mean 91 000 (±120 000) #/km-2 or 26 000 (33 000) mg/km2. Median: 48 000 #/km2 or 8 500 mg/km2. Rivers: Mean 7.0 (± 0.20) 10-3 #/L. Median: 0.36 10-3 #/L | n.i. | Manta trawl; 300m mesh | Visual sorting; FTIR on a subset. |  |
| Simon et al. 2018 | DK | WWTP | 3° treatment | 2017 | Size: Up to 600 µm | PE, PP, PEST | Raw wastewater median:: 7216 #/L or 250 ug/L Treated wastewater median: 54 #/L or 4.2 ug/L Recovery efficiency=99.3% | Blanks and spiked recovery included. | Raw WW samples filtered on-site through 10 µm stainless steel meshes. | Enzymatic and oxidative digestion; FPA-µFTIR imaging. |  |
| Browne et al. 2011 | West Hornsby and Hornsby Heights, NSW, AU | WWTP | 3° treatment | 2010 | n.i. | PEST, PMMA and PA | EF mean: 1 #/L | n.i. | Samples collected in glass bottles with metal caps. | Filtered and identified with Transmittance FT-IR |  |